## Slide 2
The Role of Surface Interactions on Xylella fastidiosa Initial Adhesion Stages
Mônica A.Cotta
Universidade Estadual de Campinas (UNICAMP)
Instituto de Física Gleb Wataghin, Campinas-SP, Brazil

## Slide 3
InP
Au
InP
InP
InAs
Materials Science
Semiconductor nanowires
T.Chiaramonte et al., Nano Lett (2011)
L.H.G.Tizei et al., Phys.Rev.Lett. (2011)
L.H.G.Tizei
D.S.Oliveira
Eshelby twist

## Slide 4
Scanning Probe Microscopy
A.C.Narvaez et al.,
Nanotechnol. (2009)
P.Sahoo et al.,
J.Phys.Chem.C (2011)
Electrical modes
Conductive-AFM
Kelvin Probe Force Microscopy

## Slide 5
B
D
A
C
+
Dibucaine
G.S.Lorite, T.M.Nobre, E.de Paula, M.E.D.Zaniquelli, M.A.Cotta,
Biophysical Chemistry, 139, pp. 75-83 (2009).
DBC added
into AFM
liquid cell;
“real time”
imaging
Real time imaging in solution

## Slide 6
Biological processes
IFGW:
Prof. Mônica A.Cotta
Dr. Richard Janissen
Alberto L.D.Moreau
Gabriela S.Lorite
Duber M.Murillo
Eng. João H. Clerici
IB:
Prof.Dagmar Machado
Prof. Anete Pereira de Souza
IAC/CC:
Dr.Alessandra A.de Souza
Carol Rodrigues
Dr.Juarez P.Tomaz
Univ. Ulm, Germany:
Prof. Boris Mizaikoff
Dr. Christine Kranz

## Slide 7
Xylella fastidiosa
Gram negative bacteria
~300–500 nm in diameter and 0.9–5μm in length
Slow growth rate (~6-48hs) and harmless
Several economically important diseases in citrus plants
citrus variegated chlorosis
~ USD 300million/year losses to citrus industry
First phytopathogenic bacterium with a complete genome sequence
Nature 406, 151 (2000)
Pathogenicity results from biofilm formation inside the plant xylem vessels
Blockage and consequent water stress plant starves!
http://www.cnr.berkeley.edu/xylella/
1m
176nm
-16nm

## Slide 8
Bacterial Biofilms
K. Sauer, Genome Biology 4, 219 (2003)
Biofilm Formation in 5 steps:
Pioneer bacterial cells reversible attachment to surface
Irreversible attachement (influence of EPS - extracellular polymeric substance)
(3) Cell-Cell adhesion and proliferation
(4) Mature biofilm
(5) Detachment
SPM analysis??
Large sizes
Biological sample reproducibility issues
To learn more:
“Slime City: Where Germs Talk to Each Other and Execute Precise Attacks"
Discover magazine, July-August 2009

## Slide 9
Dry biofilms
Very different profiles fractal (statistical) analysis

## Slide 10
http://rsb.info.nih.gov/ij/plugins/fraclac/FLHelp/BoxCounting.htm
Box counting techniques:
Scaling analysis
Dynamical scaling theory:
with
Fractal dimension:
To learn more:
“Fractal concepts on surface growth”
A.L.Barabási and H.E.Stanley
Cambridge Univ.Press, 1995

## Slide 11
Different biofilms BUT
similar scaling properties
Different biofilms on the same sample
Single bacteria
saturation
Biofilm structure

## Slide 12
Growth mechanisms
Diffusion limited
aggregation: Df ~2.5
Rich nutrient
conditions
or degradation
Circular shapes:
No branching
Low nutrient
conditions
Diffusion Barrier
Branching:
Biofilm architecture
EPS (~10 days)
A.L.D.Moreau et al, J.Appl.Phys. (2009)
Eden-like models:
Df ~2.7
100 mm
100 mm
100mm

## Slide 13
K. Sauer, Genome Biology 4, 219 (2003)
Reversible adhesion:
Electrostatic nature
Irreversible adhesion:
Chemical nature
Initial adhesion stages

## Slide 14
SPM & IR – Glass surfaces
Conditioning film due to culture medium:
changes in hydrophobicity
Live Bacteria grown inside AFM
liquid cell at 28C
ATR- IR
G.S.Lorite et al., Journal of Colloid and Interface Science 359 (2011) 289–295
Dry samples (cells around BF, 7 days)
Boris Mizaikoff and Christine Kranz

## Slide 15
Different surfaces
Si
AC
EC
Silicon
Ethylcellulose
Cellulose acetate
Si:
Defined edges
Large BFs
Large number of BFs
Enhanced adhesion and higher development rates for X. fastidiosa biofilm growth on Si surface than EC and AC surfaces
G.S.Lorite, submitted (2012)

## Slide 16
Kelvin Probe Force Microscopy (KPFM)
Acetate
Cellulose
(AC)
Ethyl
Cellulose
(EC)
Topography
Surface potential

## Slide 17
Surface Potential – Si as reference
EC: more porous film, Si surface (microscopically) exposed

## Slide 18
Si - Contact with PW

## Slide 19
Cellulose - Contact with PW
G.S.Lorite et al, APL (under review, 2012)

## Slide 20
Conditioning film – PW on substrate
Biofilm development:
optical/electron microscopy + gene expression (cellulases)
Surface Potential
Biofilm development rate
Si +
(reference)
Si +

## Slide 21
Force spectroscopy
Tip functionalization XadA1 adhesine
PBS buffer
offset
control
AC
AC
Surface
Si cantilever
Protein

## Slide 22
Force spectroscopy
AC
AC
Force (nN)
Sequence of measurements
Si
EC
#1
#2

## Slide 23
Force spectroscopy
Specific binding to AC surfaces less likely than for Si and EC
SP + force spectroscopy: different shapes of biofilms
AC
AC
AC
AC
G.S.Lorite et al., under review, 2012

## Slide 24
Back to KPFM
Surface Potential
Biofilm development rate
Si +
(reference)
Si +
Au +PW
Au (-140)mV

## Slide 25
Bacteria close to BF edges:
Experimental Identification
Capsular
EPS
EPS
around
the cells
EPS cap
layer
Duber Murillo, unpublished (2012)
Topography
Surface Potential
Phase
7 days
14 days
21 days
7 days
14 days
21 days

## Slide 26
New features?
7 days
14 days
21 days
Bacterial Poles??
Topography
Surface Potential
Phase

## Slide 27
Role of cell edges on adhesion?
With C.Lenz, INCT on Biophotonics
Xylella with GFP:

## Slide 28
Back to semiconductors…
 | MCE [ng/ml] | NsR [ng/ml] | SeR [ng/ml] | SaR [ng/ml]
40bp DNA | 4 (s= 2) | < 30 (1pM) | 30 ~ 715 | > 715
Xylella fastidiosa | 18 (s= 9) | < 34 (1.9nM) | 34 ~ 250 | > 250
Citrus Tristeza Virus | 32 (s= 16) | < 60 (2.3nM) | 60 ~ 340 | > 340
Uniform & higher fluorescence signal
Excitation: 633nm
Emission: 639-758nm
Excitation: 633nm
Emission: 640-700nm
Autofluorescence
Fluorescence of DNA-Atto647N
5µm
3µm
Autofluorescence
A.L.D.Moreau, Biosensor and Bioelectronics (2012)
R.Janissen (2012)

## Slide 29
Conclusions
Quantitative measurements of important biological parameters:
Roughness
Hidrophobicity
Electrostatic character
Surface modification
for different materials on which Xyllela fastidiosa can grow
hydrophilic surfaces
Biology: Non-specific interaction between cell and surface
  Adaptation mechanism to compensate for variability in
  plant xylem??

## Slide 30
Nanopoem by
L.H.G.Tizei and
Daniel Ugarte
Knowledge but with imagination…
FEG/STEM alignment:
Poem by
Arnaldo Antunes
“small infinite"
InP NW

## Slide 31
Financial Support
Notes: 31
31

## Slide 32
Thank you!!